# Text boxes

# Floorcoverings

# NBS & Gradus Specifications

Gradus Carpets, Park Green, Macclesfield, Cheshire SK11 7LZ England UK  Tel: 01625 428922  Fax: 01625 433949

www.gradusworld.com

Data Sheet:   (sheet 1 of 1)   04/03/08

Predator (Tile)

Gradus is a member of NBS Plus, providing a comprehensive library of pre-written specifications supported by guidance notes. The NBS specification for Predator (Tile) is shown below, plus a detailed Gradus specification and profile description to ensure the correct specification is maintained. For further information on NBS contact NBS Services on 0191 232 9594.

NBS Specification

M50 Rubber/ plastics/ cork/ lino/ carpet tiling/ sheeting.

15 CARPET TILING, 25 CARPETING, 130 CARPET TILING, 170 CARPETING

Manufacturer: Gradus Carpets, Park Green, Macclesfield, Cheshire, SK11 7LZ.

Tel: 01625 859000 Fax: 01625 850352

Website: www.gradusworld.com   Email: sales@gradusworld.com

Reference: Gradus Predator

Type: Tufted Loop Pile Tile

Gradus Detailed Specification

Manufacturer: Gradus Carpets, Park Green, Macclesfield, Cheshire, SK11 7LZ.

Tel: 01625 859000 Fax: 01625 850352

Website: www.gradusworld.com   Email: sales@gradusworld.com

Reference: Gradus Predator

Type:  Tufted Loop Pile Tile

Construction: Tufted Loop Pile

Surface Yarn: ECONYL® Regenerated SDN

Dimensions/backing:  500mm x 500mm Bitumen Backed

Pile Thickness:  3.5mm

Total Carpet Thickness: 6.5mm

Primary backing: Synthetic Non-Woven

Colours: Available in 19 colourways

Warranties: 10 year wear warranty, 10 year anti-static warranty

Consult with Gradus Carpets for technical literature and to obtain samples. Gradus Carpets can also provide a design and specification advisory service and it is recommended that they are consulted early in the design process.

Installation Instructions;

500mm x 500mm Carpet Tiles, recommended adhesive.  F. Ball & Co.  01538 361633.  Product F41

All carpet should be laid in accordance with BS5325:2001 Installation of textile floorcovering.

For further installation advice, please contact Gradus Technical Services 01625 428922

Description

Predator

Predator is a durable loop pile carpet available in both tile and broadloom formats.  It offers a stylish hardwearing solution suitable for most commercial environments.