# Text boxes

Installation Guidelines

# Accessories

Data Sheet:   (sheet 1 of 1)   January 2015 DT/LB

PVC Wetroom Transition Strips

These installation guidelines apply to the following Gradus profiles: WTS1, WTS2, WTS3

Profiles should always be allowed to acclimatise for 24 hours prior to installation at an ambient temperature of 18o Celsius. Always use a two-part epoxy adhesive where surrounding floor finishes will become wet in use.

Shower trims are installed prior to the surrounding floorcoverings.

- Ensure that all surfaces to which the profile is to be fixed are sound, dry, flat and free from any contaminants.

- Where profiles meet vertical faces they should be neatly cut to minimise the risk of any water ingress below the shower trim.

- Apply one of the recommended adhesives listed below and follow the manufacturer’s instructions for application.

- Bring both surfaces together and apply even pressure along the shower trim length ensuring any air bubbles are removed and full contact is made with the floor. Ensure the trim is firmly fixed prior to the installation of surrounding floorcoverings.

- Linear joints on either side of the shower trim must be hot welded using the floorcovering manufacturer’s recommended weld rod or sealed using a waterproof mastic or PVC cold weld .

- Joints that meet vertical surfaces at either end of the trim should be sealed using a waterproof mastic.

- Where shower trims are butt jointed together then use a PVC cold welding system before installing the trims.

Recommended adhesive products for PVC wetroom transition strips

Gradus Limited provides this information only as guidance and the legal responsibility for the supply and performance of the adhesives listed below shall remain the sole responsibility of the relevant manufacturer.

By providing this information, Gradus Limited does not imply any equivalents between each of the different manufacturers’ products, or that other products would prove unsatisfactory.  However, use of adhesives not recommended by Gradus should be supported by a guarantee from the adhesive supplier.

Application of the named adhesive must be actioned in strict accordance with the relevant manufacturers’ instructions.

Gradus do not recommend the use of spray adhesives.

If you have any queries regarding adhesives, please contact the adhesive manufacturer directly.

| Manufacturer | Product Reference | Contact number | Website |
| --- | --- | --- | --- |
| F. Ball and Co. Ltd | F84 | +44 (0) 1538 361 633 | http://www.f-ball.co.uk/ |
| Tremco | MT440, SF115 | +44 (0) 1942 251400 | http://www.tremco-illbruck.co.uk/ |
| UZIN | KR430 | +44 (0) 1788 530 080 | http://www.uzin.co.uk/ |

Gradus Accessories, Park Green, Macclesfield, Cheshire SK11 7LZ England UK  Tel: 01625 428922  Fax: 01625 433949

www.gradusworld.com

08/13/DT