Technical Data Sheet

# Accessories

Anti-Slip Primer for Safety Track

Data Sheet:   (sheet 1 of 2)   21/11/11

Description

Safety Track is a single component, high performance, solvent borne contact adhesive based on polychloroprene rubber. The product is specially formulated for use in applications which require the adhesive to have a high level of heat resistance and to a high viscosity, which minimizes penetration on porous substrates while remaining brushable for ease of application.

It was developed as a multi-purpose contact and laminating adhesive and is particularly suitable for the bonding of the more rigid, porous substrates such as chipboard, polyurethane foams,  etc and is very effective laminating plastic materials. The product can also be used to bond GRP and other plastics, wood, cork, leather, rubber.

It has proven to be effective when bonding polypropylene but is not suitable for bonding expanded polystyrene foam and patch testing is recommended before use with un-backed PVC.

It is designed to be manually applied by brush, serrated spreader, spatula etc or in certain applications the product can be sprayed after diluting with a suitable solvent.

Outstanding Features

- Easily applied by brush, serrated spreader, spatula

- Fast drying – handling strength 10 to 40mins, full cure 24 to 48hrs

- Excellent adhesion to most commonly encountered substrates

- High bond strengths

- High temperature resistance	-	up to +120°C

Applications

- Laminating		-	Wood to metal

- Plastic to wood

- Construction		-	Flooring

- Panelling

- Plastics fabrication

Gradus Accessories, Park Green, Macclesfield, Cheshire SK11 7LZ England UK  Tel: 01625 428922  Fax: 01625 433949

www.gradusworld.com

Gradus Accessories, Park Green, Macclesfield, Cheshire SK11 7LZ England UK  Tel: 01625 428922  Fax: 01625 433949

www.gradusworld.com

Anti-Slip Primer for Safety Track

Data Sheet:   (sheet 2 of 2)   21/11/11

Technical Data Sheet

# Accessories

##### Directions for use

Ensure that surfaces to be bonded are sound, clean and free from grease, dirt, dust and any other contamination, it is not normally necessary to abrade the surface before bonding. To ensure best cleaning results use NovaBond Surface Cleaner. Foam based substrates should be checked for contamination by mould release or cutting agents.

When using as a “contact adhesive” Anti-Slip Primer should be applied as a thin uniform film by brush or serrated spreader etc to both substrates and the adhesive left to dry for 10 to 40 minutes before assembly when immediate “grab” will be experienced.

When using as a “wet adhesive” Anti-Slip Primer should be applied as a thin uniform film by brush or serrated spreader etc to one substrate and the components assembled immediately, this method allows for a degree of movement and positioning.

After assembly, both methods, normal bonding pressure of 15-20 psi, depending on the compression strength of the substrates, should be applied. Sufficient bond strength should be developed after the initial 10 to 40 minutes, full curing will develop over 48hrs, depending on ambient temperature and materials being bonded.

Typical Characteristics

Appearance		:	Beige opaque liquid

Chemical base		:	Polychloroprene rubber

Solvent(s)		:	Aliphatic blend

Viscosity @ 20C	:	3500 to 4500cPs

SG @ 20C		:	0.82

Solids content		:	>25%

Temperature range	:	Up to +120C

Coverage		:	4 to 6m2/ltr

For further information contact Gradus Technical Support on 01625 428922